## Slide 1
Second part:
Semiconductor quantum dots and Coulomb blocade
for single-electron devices
4. Coulomb blocade in conducting island: principle
5. Electronic structure of semiconductor quantum dot
6. Single electron tunneling: I-V characteristics
* Tunnel transfer hamiltonian
* Metallic island
* Semiconductor island

## Slide 2
4. Coulomb blocade in conducting island: principle

## Slide 3
The quantum capacitor
insulator
* Classical capacitor:
Electrostatic energy in the capacitor:
Displacement Current:
(no charge flow through the insulator)
* Quantum capacitor:
insulator
island
tunnel junction
C
nanometer island
Voltage
Coulomb blocade
Notes: In a classical condensator the change of charge is just due to a displacement of electrons in the electrodes. It is not associated with a discrete number of electrons. There is not any flow of electron through the insulator and the granular (discrete) nature of the charge is not apparent.
The discrete nature of the charge may become apparent in very small conductors, if the associated capacitance is sufficiently small that the charging energy due to a single electron becomes comparable to or higher than the thermal energy.
The idea is thus to use QD
The charge in the island can only change step by step, when the voltage source is able to provide the required energy for an electron to transfer into the dot by tunneling through the tunnel junction.

## Slide 4
The double tunnel junction structure
quantum dot
tunnel oxide
island (or quantum dot) weakly coupled to to two leads to an external circuit via 2 tunnel junctions
Tunnel Junction
Resistance
Capacitance
and/or
 control of the current electron by electron
jonction tunnel J1
island
jonction tunnel J1

## Slide 5
The MIMIM structure
Metal / Insulator / Metal / Insulator / Metal structure
metallic island  quantization effects are neglected
jonction tunnel J
island
jonction tunnel J'

## Slide 6
The MIMIM structure: electrical modelling
Basic equations:
Calculation of the total energy E of the system:
potential (electrostatic)
energy
work done by the
voltage source
* Potential energy:
@ a single electron tunneling through
J1 or J2 is possible only if it leads to
a lower total energy
Basic idea:
i.e. with Ceq = C1 + C2 :


## Slide 7
The MIMIM structure: electrical modelling
* Work done by the source:
with
 tunneling out the island via J2:
n1
n2
n
J2  resistance
J1  capacitance
The voltage source compensate this charge variation by providing Q1
For n2 electrons the source provide the work:
 tunneling in the island via J1:
For n1 electrons the source provide the work:
J1  resistance
J2  capacitance

## Slide 8
Coulomb blocade
The MIMIM structure: electrical modelling
* Total energy:
Finally,
* Possible transitions:
 Junction 2:
 Junction 1:
Threshold voltages:
n1  n1 + 1
n2  n2 + 1
n1  n1 - 1
n2  n2 - 1
* For n = 0:
Coulomb blocade for:

## Slide 9
The MIMIM structure: electrical modelling
-4
-3
-2
-1
0
1
2
3
4
Voltage V (e/C1)
4
3
2
1
0
-1
-2
-3
-4
-5
5
Number of electrons in the island
-4
-3
-2
-1
0
1
2
3
4
Voltage V (e/C1)
4
3
2
1
0
-1
-2
-3
-4
-5
5
Number of electrons in the island
Possible transitions in a MIMIM structure at T = 0 K
* For any n value:

## Slide 10
The MIMIM structure: electrical modelling
* Dynamical behaviour:
The current through a tunnel junction may be defined as a function of the the tunneling frequency :
Considering the tunnel junction as a resistance Rt :
Starting from n = 0, the current is associated with
the total time needed for the electron to go through
both junctions of the MIMIM structure:
which correspond to the variation of potential energy :
Coulomb energy
where
Voltage (e/2C1)
Current (e/2Rt1C1)

## Slide 11
The MIMIM structure: electrical modelling
* Limitations of the model and parasitic effects:
1. Temperature
thermal energy not included in the energy balance defining the tunneling thresholds
condition of validity:
2. Knowledge of electrical parameters
C ? Rt ? Voltage dependence ? ….
3. Parasitic charges
Modification of the apparent charge in the island by q0
q0 = 0
q0 = 0.25 e
q0 = 0.5 e
Voltage (e/2C1)
Current (e/2Rt1C1)

## Slide 12
The Single Electron Transistor (SET)
The gate electrode allows controlling
the Fermi level in the dot
Current
VGS
VDS

## Slide 13
The Single Electron Memory (SEM)
reading
writing/erasing
"1"
"0"
writing
erasing
reading
"1"
"0"

## Slide 14
Electronic structure of semiconductor quantum dots
The problem:
* Semiconductor nano crystal: quantization effect
* N electron system: electrostatic interaction
charging a small number of electrons in a small dot
Schrödinger equation to be solved:
Problem similar to the case of atoms
Hamiltonian:
kinetic energy
confinement potential
interaction between electrons
exemple: Si nanocrystal
embedded in SiO2
Baron et al., J. Cryst. Growth 209 (2000) 1004
3-7 nm

## Slide 15
The methods used in atomic physics
Approximations are required to solve the Schrödinger equation in the general case
using methods developed for atoms
* The Hatree method
- easiest method to implement
- wave function is not antisymetric
(correlations not included)
- should be limited to N = 2
* The Hatree-Fock method
(Slater determinant)
- rigorous approach for any N
- wave function is antisymetric
(correlations included)
- difficult to implement
* The Density Functional Theory (DFT)
It assumes the system can be fully described
by the electron density
- rigorous for any N
- correlations included
- less information given
only total energy
no wave function

## Slide 16
The Hartree method
if  is independent of the position:
 N individual Schrödinger equations:
system of
coupled
equations
* Total energy:
! But
and
represents the interaction of electron i with the rest of the electronic cloud of density i

## Slide 17
The Hartree method
* Case of degenerated levels:
exemple: Si nanocrystal
spin
6  valleys
gj = number of electrons on level Ej
Schrödinger equation is solved for each level:
where:
* Limitation of the model:
is not antisymetric in general
except for N = 2 (thanks to the spin part of 
Nice technique, but should be used only for N  2 !

## Slide 18
The Density Functional Theory
In this theory, the electronic states are solutions to a Schrödinger equation which depends on
the electron density rather than on the individual electron wave functions.
* Hohenberg and Kohn theorem:
1. Density as basic quantity: each observable of a quantum system in fundamental state may
be deduced from the only electronic density. In particular, this is true for the total energy E [n].
2. Variational principle: the electronic density of the fundamental state may be calculated by
using the variational principle.
 Consequences:
1.  the fundamental state is a unique function of the density
2.  if E0 is the total energy of the fundamental state with a density
then,
So, the kinetic energy, the total energy and the interaction energy are functionals of n
Hamiltonian:
kinetic energy
confinement potential
interaction between electrons
Energy:

## Slide 19
The Density Functional Theory
* Kohn & Sham equation:
are unknown functions of the density
but
arbitrary decomposition in quantities easier to calculate:
is the kinetic energy of a N electron system in the external potential without including
the interaction between electrons. T0 is thus the kinetic energy of the hamiltonian:
corresponds to the potential resulting from Poisson equation:
but this potential contains the (unphysical) self-interaction of the electron on itself
is named exchange-correlation energy, defined by:
- correction of kinetic energy
- correction of self-interaction
- correlation between electrons
which includes:

## Slide 20
The Density Functional Theory
The problem is changed but not solved yet: we do not have determined
If we assume it is known:
Using variational principle, we have to find the density n minimizing the total energy E[n]
with the following condition (normalisation of n):
where
is equivalent to
1 system of N interacting electrons under
Vext
1 system of N independent electrons under
Veff = Vext + Vcoul + Vxc
 n is solution of:
strictly speaking, are not related to real energy states
 they only are tools of calculation to determine the density and the total energy
! But:
… The potential Vxc is still to be determined …
Kohn & Sham equations

## Slide 21
The Density Functional Theory
* Local Density Approximation (LDA):
we introduce the functional representing the exchange-correlation energy by electron
gradient expansion of Exc:
LDA: non local terms are neglected
Hedin and Lundqvist:
(but other expressions have been derived)
[J. Phys. C 4 (1971) 2064]
[J. Phys. (Paris) 33 (C 3) (1972) 73]

## Slide 22
The Density Functional Theory
* Total energy:
By summing the energies Ei obtained from Kohn & Sham equations, we have:
which is almost the same as the total energy previously defined:
Then,
Given the expression used for Vxc the total energy is finally:

## Slide 23
Summary: Hartree and DFT
In both cases the system of equations is similar:
Hartree:
DFT:
Vinter = Vcoul
Vinter = Vcoul + Vxc
The same numerical algorithm may be used in both case

## Slide 24
Central Field Approximation
Many types of QDs are spherical  use of central field approximation
* Hartee:
* DFT:

## Slide 25
Application to Si QDs
 Spherical Si QD embedded in SiO2
V
Si
SiO2
r0
r
m
r0
r

r0
r
To include the space variation of mass and dielectric constant:

## Slide 26
Chemical Potential
The use of the total energy as output quantity is not convenient for practical applications
The chemical potential is more useful since it corresponds to the Fermi energy of an electron gas
(for a large number of electrons)
For a discrete number of electrons N, the chemical potential is defined as
the variation of total energy resulting from an additional electron:

## Slide 27
The electronic structure (1D calculation)
1s & 2p
1s
Energy (eV)
Radius of quantum dot
Chemical potential as a function of quantum dot radius for N = 1 to N = 15
DFT calculation

## Slide 28
The density (1D calculation)
0
0.5
1
1.5
2
2.5
3
0
10
20
30
40
Position (Å)
1 electron
5 electrons
12 electrons
15 electrons
Density (nm-3)
r = 30 Å

## Slide 29
Comparison Hartree / DFT
0
0.5
1
1.5
2
2.5
3
10
20
30
40
50
60
Radius of quantum dot (Å)
Energy (eV)
DFT
Hartree
Results obtained using Hartree and DFT are very similar
We can use the Hartree technique, wich gives us the wave function for each electron

## Slide 30
3D calculation: influence of the shape of the dot
0
5
10
15
20
1
3
5
7
9
11
13
15
Number of electrons
Energy (eV)
sphere 1D
sphere 3D
cube
hemi-sphere
pyramid
Comparison of different shapes of dot at given volume
The 1D approximation gives good results of energy levels

## Slide 31
Influence of bias voltage
Bias potential (eV)
X (Å)
Y (Å)
bias potential
Vbias can be obtained from the
following Poisson's equation:
with

## Slide 32
Influence of gate bias: number of stored electrons
0.8
0.7
0.6
0.5
0.4
0.3
0.2
0.1
0
-0.1
Fundamental level (eV)
Fermi Level -
left electrode
Number of stored electrons
5
4
3
2
1
0
Fermi Level -
rigth electrode
0
0.1
0.2
0.3
0.4
0.5
0.6
Applied Bias (V)
3D : 3 electrons
3D : 2 electrons
3D : 1 electron

## Slide 33
Influence of gate bias on the density
Example: electron density for 1 electron (r = 6 nm)
V = 0
V = 0.2 V
V = 0.6 V
0
6.5
13
19.5
10-3 nm-3

## Slide 34
6. Single electron tunneling: calculation of current
quantum dot
tunnel oxide
V

## Slide 35
Single electron tunneling through a single barrier
E
* 1st method: (Schrödinger equation)
- calculation of the eigen states of the system
- transmission coefficient and probability current
 convenient for Coulomb blocade regime
* 2nd method: (Bardeen)
- weak coupling = perturbation
- Golden rule applies
 practically: limited to simple cases

## Slide 36
The tunnel transfer Hamiltonian
E
left electrode
right electrode
barrier of weak transparency
which can be considered
as a perturbation
l
r

## Slide 37
The tunnel transfer Hamiltonian
Probability per unit of time for an electron to have a tunnel event
from a state kL of the left electrode to a state kR of the right electrode:
Total probability per unit of time:
Current:
Matrix element (Bardeen):
surface of the barrier

## Slide 38
Current: approximation of the tunnel resistance
Equations of the previous slide yield:
where
* Approximation of low temperature:
 Fermi functions are step functions
* Approximation of low bias voltage:
weak 
where
is the tunnel resistance (hard approximation)

## Slide 39
MIM structure: decomposition in 2 hamiltonians
0
d/2
-d/2
V0
Vbar
V1
V3
0
-d/2
V0
V1
x
x
V/2
V
LL
d/2
Vbar
x
0
LR
V/2
Left electrode
Right electrode
+

## Slide 40
MIM structure: wave functions
WKB approximation in the barrier:
otherwise
normalisation:
… and similar results for the right electrode
 straightforward calculation of transition rates and current

## Slide 41
Current: comparison of the methods (MIM structure)
Barrier Thickness : 20 Å
T = 300 K
Tunnel Hamiltonien
Exact calculation
Tunnel resistance
0 10
0
5 10
-11
1 10
-10
1.5 10
-10
0
0.2
0.4
0.6
0.8
1
Current (pA)
Voltage (V)

## Slide 42
Transition rate and Coulomb blocade
L  Dot
Dot  R
left electrode
right electrode
R  Dot
Dot  L
insulator
tunnel junction
metal
dot
insulator
tunnel junction
metal
3D generalisation: assuming wave planes in y and z directions
(of previous assuming E << V1 + Vbar
calculations) L = volume of left electrode
R = volume of right electrode

## Slide 43
Transition rate and Coulomb blocade
* electrode  dot:
* dot  elec:

## Slide 44
Possible simplification: orthodox theory
@ first approximation: low temperature (Fermi functions = step functions)
@ second approximation: low voltage ( tunnel resistance)

## Slide 45
Calculation of current: master equation
probability to have N electrons in the dot at time t
probability to havea transition between t and t + dt
The probability to have N electrons at t + dt is:
Equation of evolution (1st order):

## Slide 46
Calculation of current: master equation
General case (for a number of electrons between –Nmax and +Nmax): matrix equation
where,
Current through a given junction (e.g. right junction):

## Slide 47
Calculation of current: Monte Carlo
Exactly the same idea as for the Monte Carlo method for solving the Boltzmann equation
collision  tunneling event
time of free flight  time without tunneling event
 series of "free flights" interrupted by tunneling events
 in this case the tunneling event i is selected
0
1
for a set of T possible tunneling events:
using 2 random numbers R1, R2 :

## Slide 48
Application to MI-Si-IM structures
Si quantum dot
V
metallic dot:
semiconductor dot:
number of free
places on the level
number of electrons
on the level
where M is numerically calculated using the wave functions
obtained from the Hartree method
The master eaquation and the Monte Carlo method may apply
as for metallic island

## Slide 49
Current: influence of dot size
radius = 30 Å hL = 15 Å hD = 12 Å
T = 4.2 K
0
20
40
60
80
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
Voltage (V)
Current (pA)

## Slide 50
Current: influence of dot radius
0
20
40
60
80
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
Voltage (V)
Current (pA)
Radius : 30 Å
Radius : 40 Å
Radius : 50 Å
hL = 1.5 nm ; hR = 1.2 nm
Negative
differential
resistance
(due to the localisation
of electrons near a
dot edge)

## Slide 51
Current: influence of dot radius
V = 0
V = 0.2 V
V = 0.6 V
left electrode
right electrode
R  Dot
Dot  L
Dot  L
R  Dot
electrons escape from the dot more rapidly that they enter the dot

## Slide 52
Influence of Temperature
0
20
40
60
80
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
Voltage (V)
Current (pA)
T=30 K
T=300 K
radius = 40 Å hL = 15 Å hD = 12 Å